## Slide 1
Characterization and Remediation of Iron(III) Oxide-rich Scale in a Pipeline Carrying Acid Mine Drainage at Iron Mountain Mine, California, USA
Kate Campbell1, Charles Alpers2, D. Kirk Nordstrom1, and Alex Blum1
1USGS, Boulder, CO
2USGS, Sacramento, CA

## Slide 2
Pipe scale in AMD pipeline
Pipe scale causes clogging and requires costly clean-out every 2-4 years
Introduction

## Slide 3
Pipelines and water treatment at IMM
Introduction

## Slide 4
Influent water to pipelines
pH = 0.5
Fe = 12,000 mg/L
Sulfate = 49,000 mg/L
pH = 2.6
Fe = 1,400 mg/L
Sulfate = 7,000 mg/L
Richmond
PW3
Introduction

## Slide 5
Water and Scale Sample Collection
Introduction

## Slide 6: Research Objectives
Characterize water chemistry and pipe scale composition
Identify biogeochemical processes leading to scale formation
Identify strategies to prevent or retard scale formation in the pipeline
Introduction

## Slide 7
Pipeline Water Chemistry
Site name | pH | Fe(T) | Fe(II) | Fe(III) | Sulfate
 |  | mg/L | mg/L | mg/L | mg/L
PW3 | 2.62 | 1460 | 1440 | <40 | 6890
SS12 | 2.63 | 1400 | 1400 | <40 | 6690
SS10 | 2.71 | 1390 | 1320 | 70 | 6480
SS8 | 2.73 | 1360 | 1040 | 320 | 6820
SS6 | 2.74 | 1360 | 1060 | 300 | 6770
Fe(II) oxidation and Fe(III) precipitation
Portal
downstream
Introduction  Objective 1

## Slide 8
Characterization of Pipe Scale
XRD, SEM
Wet chemical extractions
Total elemental digestion
C and N analysis (biomass)
deionized water
0.2M ammonium oxalate
0.5M HCl
0.5M HCl
0.5M hydroxylamine HCl
Least aggressive
Most aggressive
Schwertmannite (Fe8O8(OH)6SO4) and Goethite (FeOOH) reference compounds
Microbial community
(16S rRNA by 454-pyrosequencing)
Fe oxidizing bacteria (MPNs)
Introduction  Objective 1

## Slide 9
Bulk mineralogy is similar in all scale:
Primarily Schwertmannite [ideal composition: Fe8O8(OH)6SO4] with minor Goethite [FeOOH]
Goethite
Schwertmannite (broad peak) + goethite
Sharp peaks = corundum internal standard
SS12
SS10
SS8
SS6
Characterization of Pipe Scale
SEM courtesy of Amy Williams
Introduction  Objective 1

## Slide 10
Chart: Fe (mg/kg)
| SS12 | SS10 | SS8 | SS6
DIW | 1719.5448 | 5691.3735 | 5165.1562 | 3456.85
Ammonium oxalate | 35956.57 | 41438.29 | 40405.45 | 40683.7264
HCl | 417610.6025 | 417903.6 | 429461.85 | 405420.8
HCl/HA | 460638.56 | 468841.81 | 480415.79 | 470526.4
Chart: S (mg/kg)
| SS12 | SS10 | SS8 | SS6
DIW | 7179.422 | 10521.928 | 9721.699 | 8523.508
Ammonium oxalate | 44649.87 | 45553.3965 | 49335.071 | 43637.0801
HCl | 42964.31 | 44990.075 | 47507.98 | 41253.32
HCl/HA | 48410.677 | 49127.2175 | 51958.402 | 46052.082
Fe
S
Fe and S were dominant elements in extractions –
Schwertmannite as primary phase
Similar amounts of Fe and S extracted in all 4 scale samples –
Bulk mineralogy is similar along the pipeline
Characterization of Pipe Scale
Introduction  Objective 1

## Slide 11
Chart: % by weight
| SS12 | SS10 | SS8 | SS6
%C | 1.1277 | 0.58133 | 0.523 | 0.504
%N | 0.15833 | 0.099667 | 0.089667 | 0.072
Phosphate-extractable cells also highest in SS12
Most Probable Number (MPNs) for iron oxidizing bacteria
Biomass decreases along pipeline
Total C and N
~0.2m
SS12
Characterization of Pipe Scale
Introduction  Objective 1
Chart: mg/kg
| SS12 | SS10 | SS8 | SS6
Al | 1134.7544 | 853.7035 | 617.2189 | 486.2819
Ca | 166.4 | 81.6204 | 73.2183 | 50.4126
Cu | 622.5427 | 203.5995 | 155.4457 | 309.4092
Zn | 117.1115 | 81.1305 | 78.9045 | 80.0135
Certain trace elements decrease along pipeline
Notes: Plastic pipe
Macroscopic biomass

## Slide 12
Scale Microbial Community (16S)
Chart: 
| SS12 | SS6
Acidobacteriales | 0.064203 | 0
Holophagales | 0.0047518 | 0.2208
Acidobacteria;c | 0.0052798 | 0.0016895
Acidimicrobiales | 0.025554 | 0.0015839
Actinobacteria;Other | 0.0001056 | 0.0062302
Frankiales | 0.014361 | 0.00052798
Micrococcales | 0.014784 | 0.0036959
Propionibacteriales | 0.058184 | 0.006547
Coriobacteriales | 0 | 0.011193
Thermoleophilia;Other | 0 | 0.019852
candidate division | 0.00042239 | 0.012672
Ignavibacteriales | 0.013622 | 0.028194
Dominant classifications:
Spirochaetales
Xanthomonadales
Burkholdariales
Acidithiobacillales
Nitrosprales
Holophagales
Chloroflexi
Propionobacteriales
Acidibacteriales
Thermoplasma
Diverse microbial community
Different community up-and down-stream
Many groups with known Fe oxidizers and other C,N metabolisms
Introduction  Objective 1
Notes: 16S 454-pyrosequencing

## Slide 13
Research Objective 1
  Fe(II) is oxidized to Fe(III) in the pipeline, resulting in scale precipitation
  Scale mineralogy: schwertmannite with trace amounts of goethite, jarosite
  Biomass and trace elements in scale decrease along the length of the pipeline
  Microbial community is diverse and is different between upstream and downstream scale
Introduction  Objective 1

## Slide 14
Iron(II) oxidation at pH <3:
Abiotic oxidation is slow…
… but microbially-mediated Fe(II) oxidation has been well-documented
Acidithiobacillus, Leptosprillium, Ferroplasma, Sulfobacillus, Acidimicrobium…
Introduction  Objective 1  Objective 2
Research Objective 2: biogeochemical mechanisms

## Slide 15
Batch experiments:
Unfiltered
PW3
water
Water only = Biotic Fe(II) oxidation
Water + scale = Biotic Fe(II) oxidation, effect of scale
Control = Abiotic Fe(II) oxidation
0.1μm filtration
Research Objective 2: biogeochemical mechanisms
Introduction  Objective 1  Objective 2

## Slide 16
Fe(II) oxidation is a biotic process
Presence of scale impacts iron oxidation rates
Chart: Dissolved Fe(II)
| 0.0 | 17.0 | 25.5 | 34.5 | 45.0 | 53.0 | 61.0 | 69.0 | 76.5 | 84.0 | 91.5 | 99.0 | 112.0 | 135.0 | 180.0 | 213.0
Control 1 | 24.8196 | 24.7983 | 24.4299 | 25.3384 | 24.6498 | 24.3699 | 24.1591 | 25.2003 | 23.4008 | 23.7384
control 2 | 24.8196 | 25.2006 | 24.1925 | 25.0646 | 24.2535 | 24.5105 | 24.2104 | 23.7606 | 23.2873 | 23.7467
water only 3 | 24.9214 | 25.38 | 23.7194 | 22.8083 | 22.4699 | 20.5675 | 16.5247 | 10.7895 | 4.7252 | 0.13669
water+ scale 3 | 24.1246 | 22.2753 | 20.9716 | 20.0017 | 17.6757 | 15.6976 | 13.1119 | 9.2553 | 4.5731 | 0.13746
Abiotic controls
Unfiltered water
Unfiltered water + scale
Microbial Iron(II) Oxidation
Introduction  Objective 1  Objective 2

## Slide 17
Introduction  Objective 1  Objective 2
4Fe2+ + O2 + 4H+ → 4Fe3+ + 2H2O
Microbial Fe(II) oxidation
Iron oxidation = increase pH
Iron precipitation = decrease pH
Iron precipitation is “seeded” by scale
Precipitate formed in water only condition is Schwertmannite
Unfiltered water
Unfiltered water + scale
Abiotic controls
Fe(III) hydrolysis/polymerization
Schwertmannite precipitation
Fe3+ + H2O → FeOH2+ + H+
8Fe3+ + SO42- + 14H2O → Fe8O8(OH)6(SO4) + 22H+
Chart: pH
| 0.0 | 8.5 | 17.0 | 25.5 | 34.5 | 45.0 | 53.0 | 61.0 | 69.0 | 76.5 | 84.0 | 91.5 | 99.0 | 112.0 | 135.0 | 180.0 | 213.0 | 308.0 | 400.0 | 760.0
control 1 | 2.62 | 2.617 | 2.614 | 2.61 | 2.604 | 2.619 | 2.607 | 2.605 | 2.611 | 2.622 | 2.619 | 2.618 | 2.606 | 2.617 | 2.611 | 2.609 | 2.623 | 2.626
water only 1 | 2.708 | 2.624 | 2.631 | 2.64 | 2.643 | 2.688 | 2.709 | 2.753 | 2.8 | 2.773 | 2.613 | 2.556 | 2.49 | 2.447 | 2.429 | 2.398 | 2.398 | 2.35 | 2.349 | 2.31
water + scale 3 | 2.621 | 2.492 | 2.44 | 2.423 | 2.412 | 2.406 | 2.379 | 2.379 | 2.38 | 2.377 | 2.337 | 2.283 | 2.252 | 2.238 | 2.217 | 2.193 | 2.195 | 2.213 | 2.217 | 2.211
Microbial Iron(II) Oxidation

## Slide 18
Chart: time (hours)
| 0.0 | 8.5 | 17.0 | 25.5 | 34.5 | 45.0 | 53.0 | 61.0 | 69.0 | 76.5 | 84.0 | 91.5 | 99.0 | 112.0 | 135.0 | 180.0 | 213.0 | 308.0
experimental pH - no scale | 2.699 | 2.636 | 2.623 | 2.637 | 2.645 | 2.697 | 2.711 | 2.763 | 2.799 | 2.74 | 2.633 | 2.557 | 2.492 | 2.459 | 2.436 | 2.395 | 2.4 | 2.371
modeled pH - no scale | 2.615 | 2.6157 | 2.6175 | 2.6224 | 2.6353 | 2.666 | 2.7212 | 2.7764 | 2.5859 | 2.5281 | 2.4952 | 2.4761 | 2.4643 | 2.4563 | 2.4506 | 2.4462 | 2.4426 | 2.4395 | 2.4369 | 2.4346 | 2.4326 | 2.4307 | 2.4291
Batch model: water only condition
Microbial Fe(II) oxidation kinetics
Kinetic schwertmannite precipitation
Dissolved Fe(III) polymer included
Chart: Fe(II) (M)
| 0.0 | 25.5 | 34.5 | 45.0 | 53.0 | 61.0 | 69.0 | 76.5 | 84.0 | 91.5 | 99.0 | 112.0 | 135.0 | 180.0 | 213.0 | 308.0
 | 0.024921 | 0.02538 | 0.023719 | 0.022808 | 0.02247 | 0.020568 | 0.016525 | 0.010789 | 0.0047252 | 0.00013669
 | 0.02492 | 0.024902 | 0.024854 | 0.024723 | 0.024364 | 0.023409 | 0.021003 | 0.015794 | 0.0080392 | 0.0023589 | 0.00048443 | 8.9277e-05 | 1.6092e-05 | 2.8886e-06 | 5.188e-07 | 9.3292e-08 | 1.6761e-08 | 3.2432e-09 | 6.0288e-10 | 1.015e-10 | 1.7933e-11 | 3.2467e-12 | 6.4083e-13
Chart: time (hours)
| 0.0 | 25.5 | 34.5 | 45.0 | 53.0 | 61.0 | 69.0 | 76.5 | 84.0 | 91.5 | 99.0 | 112.0 | 135.0 | 180.0 | 213.0 | 308.0
 | 0.027035 | 0.027004 | 0.026716 | 0.026403 | 0.02592 | 0.023727 | 0.020892 | 0.020574 | 0.020851 | 0.020491 | 0.019499 | 0.019336 | 0.01885 | 0.018216
 | 0.02702 | 0.027019 | 0.02702 | 0.02702 | 0.02702 | 0.02702 | 0.02702 | 0.02702 | 0.022108 | 0.019715 | 0.018715 | 0.018341 | 0.018163 | 0.018057 | 0.017983 | 0.017926 | 0.01788 | 0.017842 | 0.017809 | 0.017781 | 0.017755 | 0.017732 | 0.017712
Introduction  Objective 1  Objective 2
Notes: Instead of jarosite, schwertmannite
Not just adding parameters – we are fitting as much as possible to data

## Slide 19
Chart: time (hours)
| 0.0 | 8.5 | 17.0 | 25.5 | 34.5 | 45.0 | 53.0 | 61.0 | 69.0 | 76.5 | 84.0 | 91.5 | 99.0 | 112.0 | 135.0 | 180.0 | 213.0 | 308.0
experimental pH - with scale | 2.642 | 2.51 | 2.449 | 2.428 | 2.414 | 2.406 | 2.372 | 2.374 | 2.384 | 2.379 | 2.36 | 2.305 | 2.261 | 2.241 | 2.219 | 2.199 | 2.199 | 2.181
modeled pH - with scale | 2.615 | 2.5671 | 2.5302 | 2.5023 | 2.4822 | 2.4692 | 2.4631 | 2.4641 | 2.4729 | 2.4895 | 2.4764 | 2.4578 | 2.4383 | 2.418 | 2.3971 | 2.3759 | 2.3548 | 2.3349 | 2.32 | 2.3091 | 2.2973 | 2.2866 | 2.2771 | 2.2612 | 2.2486 | 2.2388 | 2.2309 | 2.2247 | 2.2197 | 2.2158 | 2.2126 | 2.2101 | 2.2081 | 2.2065
Batch model: water + scale condition
Chart: Fe(II) (M)
| 0.0 | 17.0 | 25.5 | 34.5 | 45.0 | 53.0 | 61.0 | 69.0 | 76.5 | 84.0 | 99.0 | 112.0 | 135.0 | 180.0 | 213.0 | 308.0 | 400.0 | 760.0
 | 0.024125 | 0.022275 | 0.020972 | 0.020002 | 0.017676 | 0.015698 | 0.013112 | 0.0092553 | 0.0045731 | 0.00013746
 | 0.02411 | 0.023877 | 0.023589 | 0.023235 | 0.0228 | 0.022264 | 0.021608 | 0.020803 | 0.01982 | 0.018621 | 0.017168 | 0.015416 | 0.013326 | 0.010873 | 0.0080798 | 0.0050937 | 0.0023524 | 0.00064319 | 0.00010923 | 1.5692e-05 | 2.1879e-06 | 3.0378e-07 | 4.2305e-08 | 8.6394e-10 | 1.8422e-11 | 3.5369e-13 | 6.1126e-15 | 1.3185e-16 | 2.5037e-18 | 5.5737e-20 | 1.0366e-21 | 1.8164e-23 | 4.0236e-25 | 0
Chart: time (hours)
| 0.0 | 17.0 | 25.5 | 34.5 | 45.0 | 53.0 | 61.0 | 69.0 | 76.5 | 84.0 | 99.0 | 112.0 | 135.0 | 180.0 | 213.0 | 308.0 | 400.0 | 760.0
 | 0.027359 | 0.025768 | 0.025671 | 0.024844 | 0.024227 | 0.022952 | 0.0221 | 0.020517 | 0.021433 | 0.020814 | 0.020561 | 0.020283 | 0.019921 | 0.020034 | 0.021003 | 0.029089
 | 0.02731 | 0.02731 | 0.02731 | 0.02731 | 0.02731 | 0.027309 | 0.02731 | 0.027309 | 0.027309 | 0.0273 | 0.026996 | 0.026533 | 0.025929 | 0.025175 | 0.024276 | 0.023286 | 0.022354 | 0.021755 | 0.021578 | 0.021575 | 0.021575 | 0.021575 | 0.021575 | 0.021575 | 0.021575 | 0.021575 | 0.021575 | 0.021575 | 0.021575 | 0.021575 | 0.021575 | 0.021575 | 0.021576 | 0.021576
Microbial Fe(II) oxidation kinetics
Schwertmannite precipitation kinetics
Kinetic surface pH buffering reaction
Water only condition
Introduction  Objective 1  Objective 2

## Slide 20
LiCl Tracer test for 1D reactive transport model
Chart: SS12
| -1.0 | 0.0 | 0.5 | 1.0 | 1.5 | 2.0 | 2.5 | 3.0 | 3.5 | 4.0 | 4.5 | 5.0 | 5.5 | 6.0 | 6.5 | 7.0 | 8.0 | 9.0 | 10.0 | 11.0 | 12.0
 | 0.092 | 0.089 | 0.09 | 0.093 | 0.088 | 0.089 | 0.116 | 22.3 | 23.9 | 22.85 | 4.13 | 0.673 | 0.35 | 0.239 | 0.19 | 0.165 | 0.137 | 0.122 | 0.115 | 0.109 | 0.103
Chart: SS10
| 0.0 | 6.0 | 8.0 | 10.0 | 11.0 | 12.0 | 12.5 | 13.0 | 13.5 | 14.0 | 14.5 | 15.0 | 15.5 | 16.0 | 17.0 | 19.0 | 21.0 | 23.0 | 25.0 | 27.0 | 29.0
 | 0.088 | 0.091 | 0.09 | 0.087 | 0.088 | 0.014 | 5.2 | 16.3 | 20.3 | 17.4 | 7.49 | 2.61 | 1.2 | 0.7765 | 0.44 | 0.232 | 0.165 | 0.136 | 0.122 | 0.112 | 0.107
Chart: SS8
| 11.0 | 14.0 | 16.0 | 18.0 | 19.0 | 20.0 | 21.0 | 22.0 | 23.0 | 24.0 | 25.0 | 26.0 | 27.0 | 28.0 | 29.0 | 31.0 | 33.0 | 35.0 | 37.0 | 40.0
 | 0.091 | 0.09 | 0.087 | 0.092 | 0.087 | 0.09 | 0.626 | 14.6 | 15.9 | 2.99 | 1.01 | 0.5535 | 0.374 | 0.277 | 0.221 | 0.161 | 0.136 | 0.121 | 0.114 | 0.107 | 0.091
Chart: SS6
| 16.0 | 19.0 | 21.0 | 23.0 | 25.0 | 26.0 | 27.0 | 28.0 | 29.0 | 30.0 | 31.0 | 32.0 | 33.0 | 34.0 | 36.0 | 38.0 | 41.0 | 44.0 | 47.0 | 50.0
 | 0.089 | 0.09 | 0.089 | 0.089 | 0.09 | 0.091 | 0.091 | 0.091 | 0.334 | 12.6 | 15.4 | 4.28 | 1.36 | 0.685 | 0.31 | 0.205 | 0.143 | 0.12 | 0.11 | 0.103
Introduction  Objective 1  Objective 2

## Slide 21
Research Objective 2
  Iron oxidation is biotic
  Iron precipitation is “seeded” by scale
  Precipitate formed in batch experiments is similar to scale
  Batch geochemical model
    Kinetics: Microbial Fe oxidation, precipitation, surface buffering
  Field scale processes
    In situ rates of Fe oxidation
    1D reactive transport model
      test remediation strategies
      application to other sites with pipe scaling
Introduction  Objective 1  Objective 2

## Slide 22
Introduction  Objective 1  Objective 2  Objective 3
Research Objective 3 - mitigation
Mixing PW3 and Richmond waters:
Fe(II) oxidation may be hard to control
Precipitation can be prevented by decreasing pH
PHREEQC calculations of saturation index of schwertmannite
Variable Fe(III) concentrations, mixing ratios (pH)
~5% Richmond + 95% PW3
Batch experiments:
1%, 5%, 10% Richmond water, balance PW3
With and without scale (effect of pre-existing scale)
Range of Fe(III) conditions by inoculating with a microbial culture

## Slide 23
Precipitation in 1% Richmond – none in 5%, 10%
Chart: Total dissolved Fe (mM)
| 0.0 | 81.0 | 95.0 | 118.0 | 173.0 | 262.0 | 341.0
99% PW3 / 1% Richmond | 29.8149 | 25.9018 | 24.6333 | 22.722 | 22.0833 | 22.3375 | 21.1356
95% PW3 / 5% Richmond | 36.0007 | 34.7583 | 34.7164 | 34.42 | 34.1344 | 35.9281 | 36.0766 | 36.4762
90% PW3 / 10% Richmond | 45.5279 | 44.7813 | 45.2908 | 45.7142 | 44.9191 | 44.7171 | 45.8055
Chart: time (hours)
| 0.0 | 19.0 | 28.0 | 42.0 | 54.0 | 67.0 | 81.0 | 95.0 | 118.0 | 144.0 | 173.0 | 262.0 | 341.0
99/1 | 2.486 | 2.488 | 2.475 | 2.552 | 2.622 | 2.659 | 2.597 | 2.546 | 2.469 | 2.436 | 2.404 | 2.386 | 2.381
95/5 | 2.081 | 2.009 | 2.023 | 2.076 | 2.147 | 2.249 | 2.305 | 2.36 | 2.361 | 2.363 | 2.359 | 2.364 | 2.369
90/10 | 1.795 | 1.734 | 1.755 | 1.78 | 1.796 | 1.865 | 1.913 | 1.994 | 2.043 | 2.063 | 2.075 | 2.069 | 2.081
Chart: time (hours)
| 0.0 | 19.0 | 28.0 | 42.0 | 54.0 | 67.0 | 81.0 | 95.0 | 118.0 | 173.0 | 262.0
99% PW3 / 1% Richmond | 2.464 | 2.397 | 2.388 | 2.38 | 2.353 | 2.323 | 2.258 | 2.257 | 2.221 | 2.2 | 2.18
95% PW3 / 5% Richmond | 2.083 | 2.262 | 2.269 | 2.277 | 2.255 | 2.249 | 2.2 | 2.194 | 2.165 | 2.14 | 2.129
90% PW3 / 10% Richmond | 1.805 | 2.176 | 2.192 | 2.202 | 2.189 | 2.195 | 2.152 | 2.155 | 2.108 | 2.089 | 2.078
Chart: 
| 0.0 | 19.0 | 28.0 | 42.0 | 54.0 | 67.0 | 81.0 | 95.0 | 118.0 | 144.0 | 173.0 | 262.0
99% PW3 / 1% Richmond | 28.2634 | 28.0903 | 30.7983 | 29.7321 | 31.0294 | 26.0987 | 23.393 | 22.9733 | 22.3659 | 22.7639 | 22.2165
95% PW3 / 5% Richmond | 36.4581 | 44.6352 | 41.468 | 39.8168 | 40.0703 | 38.3618 | 36.3302 | 33.6479 | 32.6303 | 31.9242 | 34.1487
90% PW3 / 10% Richmond | 43.6053 | 56.3048 | 55.7284 | 56.3966 | 55.8993 | 52.7356 | 55.6979 | 50.6227 | 49.2934 | 48.9751 | 47.6824
no scale
with scale
Fe(T)
pH
Scale buffers pH to 2.1-2.2
10%
5%
1%
10%
5%
1%
Decreasing pH by mixing with Richmond effective in preventing scale formation
Pipe Scale Mitigation
Introduction  Objective 1  Objective 2  Objective 3

## Slide 24
Introduction  Objective 1  Objective 2  Objective 3  Conclusions
Fe(II) is oxidized to Fe(III) in pipeline, resulting in precipitation
Fe(II) oxidation is microbially mediated
Scale is composed of schwertmannite, with minor goethite
Presence of scale “seeds” precipitation
Mixing of Richmond and PW3 as potential mitigation strategy
  Confirm with field tests, over range of chemistry
Presence of scale strongly buffers pH
  Buffering capacity of scale and rate of scale dissolution are important considerations for other mitigation strategies
1D reactive transport model for testing biogeochemical processes, remediation strategies
    Field-scale modeling as guidance for effective planning
Conclusions

## Slide 25
Thank you for your attention!
Acknowledgements:
James Sickles (US EPA)
Amy Williams (UC Davis)
Lily Tavassoli (US EPA)
Rudy Carver (Iron Mountain Operations)
Theron Elbe (Iron Mountain Operations)
Don Odean (Iron Mountain Operations)
Gary Campbell (USGS)
JoAnna Barrell (Colorado School of Mines)
David Metge (USGS)
Deb Repert (USGS